Supplementary Materials: Effect of Synthesis Conditions of Nitrogen and Platinum Co-Doped Titania Films on the Photocatalytic Performance under Simulated Solar Light

Daryna Ihnatiuk 1,2 Camilla Tossi 1, Ilkka Tittonen 1 and Oksana Linnik 3,*

| a | b |
| --- | --- |
| c |  |

Figure S1. Absorption spectra of the films obtained by Method 1 (a) and Method 2 (b) 0.5mol%Pt -doped films: TiO2 (1), Pt-TiO2 (2), Pt-TiO2UV (3), Pt,N-TiO2 (4), Pt,N-TiO2UV (5). Emission spectra (c) of a 1000 W middle-pressure mercury lamp without (1) and with (2) the cut-off filter, the solar radiation spectrum is shown in curve (3).

| a | b |
| --- | --- |

Figure S2. Tauc plots of the films obtained by Method 1 (a) and Method 2 (b) TiO2 (1) and N-TiO2 (2) films.

Figure S3. XRD patterns of N-TiO2 films obtained by Method 1 (1) and Method 2 (2): a-anatase and b-brookite.

| N1s |  |
| --- | --- |
| Ti2p |  |
| O1s |  |

Figure S4. N1s, Ti2p and O1s XPS spectra of the N-TiO2 films obtained by Method 1 (left) and Method 2 (right).

| 1Pt-TiO2M1 | 1Pt,N-TiO2M1 |
| --- | --- |
| 1Pt-TiO2M1UV | 1Pt,N-TiO2M1UV |
| 1Pt-TiO2M2 | 1Pt,N-TiO2M2 |
| 1Pt-TiO2M2UV | 1Pt,N-TiO2M2UV |

Figure S5. Deconvoluted XPS O1s spectra of Pt and Pt,N co-doped titania films.

Table S1. Binding energy values of Pt4f XPS spectra.

| Film | Pt0 |  | Pt2+ |  | Pt0 |  | Pt2+ |  | Pt4+ |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Pt4f7/2 | Pt4f5/2 | Pt4f7/2 | Pt4f5/2 | Pt4f7/2 | Pt4f5/2 | Pt4f7/2 | Pt4f5/2 | Pt4f7/2 | Pt4f5/2 |
|  | Method 1 |  |  |  | Method 2 |  |  |  |  |  |
| 0.5Pt-TiO2 | 70.2 | 73.5 | 71.0 72.4 | 74.4 75.8 | - | - | 72.3 | 75.7 |  |  |
| 0.5Pt,N-TiO2 | 70.8 | 74.1 | 72.4 | 75.8 | 70.6 | 74.0 | 72.3 | 75.6 | - | - |
| 0.5Pt-TiO2UV | 70.7 | 74.0 | 72.5 | 75.9 | - | - | 72.4 | 75.8 | 74.2 | 77.6 |
| 0.5Pt,N-TiO2UV | 71.0 | 74.3 | 72.1 | 75.4 | 70.6 | 74.0 | 72.3 | 75.7 | - | - |
| 1Pt-TiO2 | 71.4 | 74.7 | 72.1 | 75.4 | - | - | 72.0 | 75.4 | - | - |
| 1Pt,N-TiO2 | 70.4 | 73.7 | 72.0 | 75.3 | 70.5 | 73.8 | 71.2 72.5 | 74.6 75.8 | 74.3 | 77.6 |
| 1Pt-TiO2UV | 70.3 | 73.6 | 71.1 | 74.4 | - | - | 72.3 | 75.6 | 74.3 | 77.6 |
| 1Pt,N-TiO2UV | 69.6 | 73.0 | 71.4 | 74.7 | 70.8 | 74.2 | 72.5 | 75.8 | 74.6 | 78.0 |

| (a) | (b) | (c) |
| --- | --- | --- |
| (d) | (e) | (f) |

Figure S6. (a) 1%Pt-TiO2M2; (b) 1%Pt-TiO2M1; (c) 1%Pt-TiO2M1UV; (d) 1%Pt,N-TiO2M2; (e) 1%Pt,N-TiO2M1; (f) 1%Pt,N-TiO2M1UV.